## Slide 1: Non-Steady State Corrosion by CO2
David Young
Lesson 3 Class 1
School of Materials Science & Engineering
University of New South Wales
Sydney, Australia

## Slide 2: Reaction Morphology Ferritic-Martensitic Steels
P92, Ar-50%CO2 for 150h

## Slide 3: Reaction Morphology Ferritic-Martensitic Steels
P92, Ar-50%CO2 for 150h, 550oC

## Slide 4: Carbon Distribution (GDOES)
P92, Ar-50%CO2 for 150h, 550oC
As t increases:
1.
2.

## Slide 5: Boundary Value of C Concentration
P92 and VM12 at 550°C in Ar-50%CO2

## Slide 6: Oxide-Alloy Interface
Interface moves, because ..
Alloy carbon concentration increases

## Slide 7: Non-equilibrium Boundary Condition

## Slide 8: Boundary Value of C Concentration
P92 and VM12 at 550°C in Ar-50%CO2
Equilibrium:
6.8 at. %
Equilibrium:
9.1 at. %

## Slide 9: Non-equilibrium Boundary Condition
Gas
Alloy
Oxide scale

## Slide 10: Non-equilibrium Boundary Condition
Alloy
Oxide scale

## Slide 11: Non-equilibrium Boundary Condition
THREE PROCESSES
1.
2.
3.

## Slide 12: Carbon Injection at Oxide-Alloy Interface

## Slide 13: Carbon Injection at Oxide-Alloy Interface
Carbon injection rate
Carbon removal rate

## Slide 14: Carburisation Kinetics
Parabolic (steady-state) kinetics
BUT, non steady state boundary condition!

## Slide 15: Non-equilibrium Boundary Condition
C diffusion via ferrite matrix, not the precipitates
Measured C concentration is for (matrix + precipitates)

## Slide 16
Assume local equilibrium
Use phase diagram
Apply lever rule

## Slide 17
Assume local equilibrium
Use phase diagram
Apply lever rule

## Slide 18: Precipitation of Cr7C3

## Slide 19: Precipitation of Cr7C3
(a)
(b)
(c)

## Slide 20: Precipitation of Cr7C3
(a)
(b)
(c)

## Slide 21: Precipitation of Cr7C3
EQUATIONS:

## Slide 22: Precipitation of Cr7C3
EQUATIONS:
Total C increases a lot
BUT, CC in ferrite changes little
EXPLAINS why carbon matrix diffusion
almost steady-state

## Slide 23: Solve Diffusion Equation
In matrix, conventionally,
Must modify to account for precipitation of C as carbide
Substitute

## Slide 24: Solution

## Slide 25: Test Solution at Surface
At surface, x = 0

## Slide 26: Apply to Lab Data
Prediction of increase in surface concentration good

## Slide 27: AGR Accelerated Corrosion Tests

## Slide 28: AGR Accelerated Corrosion Tests
Maximum Operating Temperature
~ 540oC

## Slide 29: Internal Carburisation
Measured volume fraction of carbide as f(position in fin)

## Slide 30: Carbide Profiles Across Fin

## Slide 31: DICTRA fit to C Curves
Fit reasonably successful
Allows prediction of time to saturation of fin withC

## Slide 32: Predict Breakaway at C Saturation

## Slide 33: SUMMARY
At low T, C very slow to equilibrate at oxide-steel surface
Surface concentration increases with time
Lab (short-term) data described using C diffusion model with injection rate boundary condition
Analytical solution possible for semi-infinite geometry
Not applicable to cooling fins on heat exchanger
Can model numerically – successfully fit C profiles
Lifetime prediction possible